## Slide 1: Măsurarea grosimii sub obstrucție Thickness Measuring Under Obstruction
Matt Davison – DakotaNDT

## Slide 2: Corrosion Grid Mapping
Cartarea coroziunii produce o rețea de măsurători distribuite pe zona țintă a activului.
Aceasta permite monitorizarea sistematică a coroziunii în timp.
Corrosion Mapping produces a grid of measurements spread out over the asset’s target area.
This allows for systematic monitoring of corrosion over time.
Year 1
Year 5
Year 10

## Slide 3: Obstrucție de suprafață / Surface Obstruction
O provocare este obstacolul de suprafață.
Adesea înregistrat în magazinul de date ca obstacol. **OBST**
Important de verificat
A challenge is the Surface obstacle.
Often logged in the data logging store as obstacle. **OBST**
Important to check

## Slide 4: Advanced Ultrasonic Techniques
Long Range UT
Phased Array S-Scan
Encoded C-Scan
Large transducer collar allows for the generation of guided waves, which can travel along 100m+ of pipeline from a single location.
PAUT transducers allow for a Sectoral scan, similar to those used in medical sonography. This is a focused technique that can cause display warping.
A grid of encoded B-Scans can be combined into a top-down view of material under test; cutting edge can even present scans in 3d.

## Slide 5: Ce-ar fi dacă am despărți transductorul? What if we split the transducer?
Pulse
Echo

## Slide 7: Experiment
Setare
Diametru sondă
Unghiul transductorului 45/60/70
Răspândirea fasciculului
Metoda de calibrat
Rezultate
Set Up
Probe Diameter
Angle of transducer 45/60/70
Beam Spread
Calibration Method
Results

## Slide 8: Verificare și configurare a sondei Probe Check and Set-Up

## Slide 9: 40mm Blocks

## Slide 10: Calculating the PCS – Probe Centre Separation (Centru de Separare a Probelor)

## Slide 11
Notes: Conclusion - Better to use Beam amplitude loss to confirm range possible.

## Slide 12: Răspândirea razelor / Beam Spread
Chart: 45 degree Amplitude drop off against PCS – 4MHz
| -22.5 | -20 | -17.5 | -15 | -12.5 | -10 | -7.5 | -5 | -2.5 | 0 | 2.5 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5 | 20 | 22.5
12.5mm 40 | 7 | 10 | 18 | 25 | 35 | 50 | 65 | 80 | 90 | 100 | 90 | 80 | 63 | 50 | 37 | 25 | 14 | 12 | 7
10.0mm 40 | 3 | 8 | 12 | 18 | 30 | 45 | 60 | 75 | 90 | 100 | 90 | 75 | 55 | 42 | 30 | 16 | 8 | 5 | 3
#REF! | 1

## Slide 13: Răspândirea razelor / Beam Spread
Chart: 45 degree Amplitude drop off against PCS – 4MHz optimised at different depths
| -22.5 | -20 | -17.5 | -15 | -12.5 | -10 | -7.5 | -5 | -2.5 | 0 | 2.5 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5 | 20 | 22.5
10.0mm 40 | 3 | 8 | 12 | 18 | 30 | 45 | 60 | 75 | 90 | 100 | 90 | 75 | 55 | 42 | 30 | 16 | 8 | 5 | 3
#REF! | 1
10mm 25mm deep | 0 | 0 | 1 | 7 | 12 | 25 | 40 | 62 | 85 | 100 | 85 | 75 | 50 | 25 | 12 | 7 | 3 | 1 | 0
10mm 15mm deep | 0 | 0 | 0 | 0 | 5 | 10 | 25 | 50 | 85 | 100 | 85

## Slide 14: Ajustarea PCS pe citirea grosimii Adjusting PCS on Thickness Reading
Notes: Adjust PCS to obtain maximum range, not as thought with beam width.

## Slide 15: Calibration - doar două puncte!
Single point, two point tested as on standard Thickness Gauge – two point only!
Cal point 1
Cal point 2

## Slide 16: Range of Measurement
45 = 7mm raise to 14mm
60 = 5.5mm raise to 11mm
70 = 5mm raise to 10mm
Reduced far surface coverage and detection of far surface indications

## Slide 17: Test 1 Simularea coroziunii / Corrosion Simulation

## Slide 18: Rezultat / Results
2
3
4
1

## Slide 19: 25mm Block
10mm Block

## Slide 20: Test 2 – Corrosion Type / Tip de coroziune

## Slide 21: Orientation Orientare și Direcție

## Slide 22: Observații / Observations

## Slide 23: Măsurarea defectelor mici, aproape de ecoul mare de la peretele din spate, poate mască semnalul, reducerea PCS-ului atenuează astfel problemele de amplitudine. Measuring small defects, near large back wall echo can mask signal, shifting the PCS reduces such amplitude issues.

## Slide 24
Cresterea câștigului poate fi necesară pentru a obține grosimea din semnale slabe din probleme de orientare a indicațiilor – de obicei 12dB conform metodei este suficient.
Increased gain can be needed to obtain thickness from low signals from indication orientation issues – usually 12dB as per method is sufficient.

## Slide 25: Concluzie / Conclusion

## Slide 26
Precizia dimensiunii este comparabilă cu TOFD
Măsurările TREBUIE să fie în intervalul de calibrare de 2 puncte Înregistrarea și redarea
ajută la scanarea celei mai subțiri părți
Funcționează – sub obstrucții pot fi măsurate!
Sizing accuracy comparable to TOFD
Measurements MUST be inside a 2 point calibration range
Recording and playback help scanning for the thinnest part
It Works – under obstructions can be measured!
Concluzie / Conclusion

## Slide 27: Pașii următori / Next Steps
Mai multe studii de teren
Intervalele transducătoare testate, diametru, frecvențe
Cineva a menționat AI?
More Field Trials
Transducer ranges tested, diameter, frequencies
Did anyone mention AI?

## Slide 28: Dual Shear Wave “DSW”
Mulțumesc – Orice întrebări?